SECTION 330130.87 - CHANGING ELEVATIONS OF MANHOLES AND DRAINAGE STRUCTURES

1. GENERAL
   * + 1. RELATED WORK SPECIFIED ELSEWHERE
          1. Earthwork: Section 310000.
2. PRODUCTS
   * + 1. MATERIALS
          1. Sewer Brick: ASTM C 32, Grade MS.
          2. Concrete Masonry Units: ASTM C 139.
          3. Mortar: ASTM C 270, Type M.
3. EXECUTION
   * + 1. ADJUSTMENTS
          1. Raise or lower the existing frames, covers and gratings of manholes, and drainage structures to the grades fixed by the Director’s Representative.
          2. Parge exterior surface with mortar when brick or masonry units are added or when the exterior surface is disturbed.
          3. Replace frames, covers or gratings damaged during the Work of the Contract.

END OF SECTION 330130.87